Phone: 440-235-1140

Manufacturers of plastic insulated wires and cables

American Wire and Cable Company

7951 Bronson Road

# Olmsted Falls, Ohio 44138

## SPECIFICATION

UL AND CSA APPROVED PVC INSULATED LEAD WIRE,

.O30 MIL WALL, BARE OR TINNED COPPER CONDUCTOR,

UL AWM 105C 600V UL STYLE 1015/1230,

90C 1000V UL STYLE 1032, VW-1,

CSA 105C AWM/TEW, FT-1

| AWG | STRANDS | NOMINAL O.D. |
| --- | --- | --- |
| 22 | 7/30 | .096 |
| 20 | 10/30 | .103 |
| 18 | 16/30 | .107 |
| 16 | 26/30 | .117 |
| 14 | 41/30 | .133 |
| 12 | 65/30 | .153 |
| 10 | 105/30 | .197 |

RoHS Compliant